Blackstone Labs Oil Analysis

EQUIPMENT MAKE: 2000 Volkswagen Golf

EQUIPMENT MODEL: 1.9L Turbo (TDI)

FUEL TYPE: Diesel & Biodiesel

OIL TYPE & GRADE: Valvoline 5W40 Premium Blue Extreme

ELEMENTS IN PARTS PER MILLION

| MI/HR ON OIL | 0 | 4700 | 10,000 |
| --- | --- | --- | --- |
| MI/HR ON Unit |  | 89,930 | 95,259 |
| Sample Date | 09/28/04 | 12/22/04 | 2/14/05 |
| ALUMINUM | 0 | 2 | 3 |
| CHROMIUM | 0 | 1 | 2 |
| IRON | 1 | 14 | 21 |
| COPPER | 0 | 2 | 3 |
| LEAD | 0 | 1 | 0 |
| TIN | 0 | 0 | 1 |
| MOLYBDENUM | 64 | 57 | 54 |
| NICKEL | 0 | 1 | 1 |
| MANGANESE | 0 | 0 | 1 |
| SILVER | 0 | 0 | 0 |
| TITANIUM | 0 | 0 | 0 |
| POTASSIUM | 0 | 0 | 2 |
| BORON | 89 | 72 | 54 |
| SILICON | 2 | 5 | 5 |
| SODIUM | 1 | 11 | 13 |
| CALCIUM | 2627 | 3328 | 2986 |
| MAGNESIUM | 9 | 103 | 85 |
| PHOSPHORUS | 851 | 1067 | 944 |
| ZINC | 957 | 1301 | 1245 |
| BARIUM | 0 | 0 | 0 |
| TBN | 13.1 | 8.2 | 3.7 |

PROPERTIES

| TEST | cST VISCOSITY @ 40 ºC | SUS VISCOSITY @ 100 ºF | VISCOSITY INDEX | cST VISCOSITY @ 100 ºC | SUS VISCOSITY @ 210 ºF | FLASHPOINT IN ºF | FUEL % | ANTIFREEZE % | WATER % | INSOLUBLES % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| VALUES SHOULD BE |  |  |  |  | 65-76 | >410 | <2.0 | 0 | <0.1 | <0.8 |
| TESTED VALUES @ 0 MILES WERE |  |  |  |  | 77.0 | 440 | - | - | 0.0 | 0.0 |
| TESTED VALUES @ 4700 MILES WERE |  |  |  |  | 82.9 | 445 | <0.5 | 0.0 | 0.0 | 0.4 |
| TESTED VALUES @ 10000 MILES WERE |  |  |  |  | 76.3 | 445 | <0.5 | 0.0 | 0.0 | 0.5 |

Virgin Oil Analysis Comments:

WILLIAM: The TBN for this unused oil was 13.1, quite a high level, and higher than most 5W/40s we

run. This oil was clean and dry and has a nice additive group that should serve your needs well. No

significant metals found. This is serviceable 5W/40 diesel-use engine oil.

4,700 Mile Analysis Comments:

WILLIAM: This is an amended report with the TBN. That sodium shouldn't be there, so we suggest

you check back with another oil sample before too much more time, to make sure it isn't from an

anti-freeze problem developing. At this low level, it could be from another source. Wear improved to

well below universal average levels, after the 4,700 mile oil use interval. Our average oil from this type

engine has 7,725 miles on it, so you have miles to give, should you decide to run your oil longer. The

TBN was strong at 8.2, showing plenty of active additive left. 1.0 is low.

10,000 Mile Analysis Comments:

WILLIAM: This is the same oil as last sample with an additional 5,329 miles use on it and we think it

has held up well. Wear increased only slightly. Most of the increase was at iron (from steel parts) and

this was to be expected. Sodium increased a little, though not enough to think you have an anti-freeze

problem, so we aren't worried about it. The TBN dropped to 3.7, from 8.2 last time. This is still a

strong reading. The insolubles were okay and no fuel dilution was found. At 95,259 total miles, we

think this engine is doing well. Try 13,000 miles on the next oil.